## Slide 1
Chart: 
| R1_DLS | R1_NTA |  | R2_DLS | R2_NTA |  | R3_DLS | R3_NTA
 | 213200000 | 250000000 | 140800000 | 100000000 | 84190000 | 65500000
 | 282900000 | 275000000 | 99760000 | 95200000 | 57240000 | 77100000
 | 281000000 | 257000000 | 109000000 | 99200000 | 52950000 | 79700000
Se-PS-NPs NTA size and concentration
Se-PS-NPs DLS size
0.25% w/w
0.7% w/w
2.7% w/w
Concentration (106 NPs/mL)
Intensity (%)
size (nm)
size (nm)
size (nm)
size (nm)
size (nm)
size (nm)
Se-PS-NPs NTA and DLS concentration
Concentration (108 NPs/mL)
(a)
(b)
(c)
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
| R1_DLS | R1_NTA | R2_DLS | R2_NTA |  | R3_DLS | R3_NTA
 | 164100000 | 113000000 | 197600000 | 180000000 | 49460000 | 72400000
 | 124300000 | 136000000 | 190100000 | 209000000 | 125500000 | 59700000
 | 135500000 | 129000000 | 205900000 | 221000000 | 94710000 | 56900000
Chart: 
| R1_DLS | R1_NTA |  | R2_DLS | R2_NTA |  | R3_DLS | R3_NTA
 | 138900000 | 163000000 | 123800000 | 127000000 | 77740000 | 71200000
 | 147300000 | 158000000 | 91560000 | 120000000 | 68700000 | 77800000
 | 173900000 | 166000000 | 129400000 | 124000000 | 61810000 | 70900000
Figure S8. Additional NTA and DLS size and concentrations distributions for replicates (R1, R2, R3) of 0.25%, 0.7%, 2.7% w/w of Se-PS-NPs; (a) NTA size and concentration distributions. Average size by NTA was 249 ± 17 nm, 253 ± 42 nm and 234 ± 27 nm for 0.25%, 0.7%, 2.7% w/w Se-PS-NPs; (b) DLS size distributions. Average size by DLS was 292 ± 42 nm, 292 ± 34 nm and 302 ± 88 nm for 0.25%, 0.7%, 2.7% w/w Se-PS-NPs. Samples with lower concentrations of nanoparticles increased the standard deviations for DLS data; (c) Comparison between NTA and DLS determined concentrations. Error bars indicate standard deviations.

## Slide 2
Raw dissolved selenium concentration after 2x dilution in 1% HNO3 (aq) determined by ICP-MS (ppb)
Time (Days)
Time (Days)
(a)
(b)
(c)
(d)
Chart: 
| 0 | 3 | 7 | 14 | 21 | 28 | 35
0.25R1 | 0.56618 | 0.4935 | 0.54276 | 0.58378 | 0.50036 | 0.48051 | 0.50882
0.25R2 | 0.59341 | 0.50322 | 0.51636 | 0.51331 | 0.46308 | 0.56586 | 0.46648
0.25R3 | 0.53147 | 0.53769 | 0.59102 | 0.50377 | 0.38542 | 0.52994 | 0.53423
Chart: 
| 0 | 3 | 7 | 14 | 21 | 28 | 35
0.7R1 | 0.56485 | 0.63553 | 0.59707 | 0.51589 | 0.73887 | 0.58911 | 0.49141
0.7R2 | 0.54273 | 0.5528 | 0.58423 | 0.58775 | 0.55212 | 0.61411 | 0.49272
0.7R3 | 0.552 | 0.51954 | 0.55807 | 0.53596 | 0.61094 | 0.50814 | 0.57548
Chart: 
| 0 | 3 | 7 | 14 | 21 | 28 | 35
BlkR1 | 0.48953 | 0.50579 | 0.47938 | 0.44186 | 0.5039 | 0.63645 | 0.50882
BlkR2 | 0.54123 | 0.38877 | 0.51668 | 0.52307 | 0.47869 | 0.49592 | 0.46648
Chart: 
| 0 | 3 | 7 | 14 | 21 | 28 | 35
2.7R1 | 0.83255 | 0.60988 | 0.63249 | 0.65174 | 0.63508 | 0.65921 | 0.55776
2.7R2 | 0.5821 | 0.62777 | 0.5902 | 0.59431 | 0.68378 | 0.70399 | 0.45962
2.7R3 | 0.62612 | 0.63381 | 0.58157 | 0.63645 | 0.65506 | 0.68632 | 0.67336
Figure S9. Raw dissolved Se ICP-MS data from 35 days leaching test experiments for 10 ppm of Se-PS-MNPs in MHRW; (a) 0.25% w/w, triplicates; (b) 0.7% w/w, triplicates; (c) 2.7% w/w, triplicates; (d) Blanks, duplicates.

## Slide 3
10 ppm exposure 0.7% w/w Se-PS-MNPs
Figure S10. Additional O-PTIR and Nano TOF-SIMS information for Figure 5. (a) Original 10x O-PTIR microscope image of a histological slice of a Daphnia magna exposed to 10 ppm 0.7% w/w Se-PS-MNPs. Emphasis is put on a section of the digestive tract. Red dotted square indicates location of the analysis; (b) O-PTIR mapping of a 96 x 85 µm region of the exposed D. magna at the wavenumber 1453 cm-1 aromatic C-H bending identifiable in polystyrene with point analysis shown by the red crosses at 30 random locations with intensities above 7 mV, with color bar shown on the right side of the image. Mapping done with a scan rate of 100 µm/s at a resolution of 0.2 µm/point with a probe power of 3% and an IR power of 17%; (c) Individual O-PTIR spectrum for each red cross in b) with small circles indicating the presence of identified Se-PS-MNPs by the sharp peaks at 1491 cm-1 and 1453 cm-1 and small triangles indicating non-confirmation of the presence of Se-PS-MNPs; (d) Nano-TOF-SIMS negative ion scan with counts for a m/z range of 0 – 100 g/mol; (e) Nano-TOF-SIMS negative ion analysis with emphasis on counts of Se- at 79.95 g/mol; (f) Nano-TOF-SIMS positive ion scan with counts for a m/z range of 0 – 100 g/mol; (g) Nano-TOF-SIMS negative ion analysis with emphasis on counts of C7H7+ at 91 g/mol.
(a)
(b)
Wavenumber (cm-1)
(c)
Chart: 
0
50
150
79.80
79.85
79.90
79.95
80.00
(d)
(e)
0
50
150
Mass [m/z]
90.0
90.5
91.0
91.5
(f)
(g)
Negative ion scan
Negative ion scan, Se-
Positive ion scan
Positive ion scan, C7H7+
Microscope image
1453 cm-1 map
Full spectra analysis
O-PTIR
TOF-SIMS
100
Confirmed Se-PS-MNPs peaks
Unconfirmed Se-PS-MNPs peaks
100

## Slide 4
1 ppm exposure 0.7% w/w Se-PS-MNPs
Figure S11. Additional O-PTIR and Nano-TOF-SIMS information for Figure 5. (a) Original 10x O-PTIR microscope image of a histological slice of a Daphnia magna exposed to 1 ppm 0.7% w/w Se-PS-MNPs. Emphasis is put on a section of the digestive tract. Red dotted square indicates location of the analysis; (b) O-PTIR mapping of a 96 x 85 µm region of the exposed D. magna at the wavenumber 1453 cm-1 aromatic C-H bending identifiable in polystyrene with point analysis shown by the red crosses at 30 random locations with intensities above 7 mV, with color bar shown on the right side of the image. Mapping done with a scan rate of 100 µm/s at a resolution of 0.2 µm/point with a probe power of 3% and an IR power of 17%; (c) Individual O-PTIR spectrum for each red cross in b) with small circles indicating the presence of identified Se-PS-MNPs by the sharp peaks at 1491 cm-1 and 1453 cm-1 and small triangles indicating non-confirmation of the presence of Se-PS-MNPs; (d) Nano-TOF-SIMS negative ion scan with counts for a m/z range of 0 – 200 g/mol; (e) Nano-TOF-SIMS negative ion analysis with emphasis on counts of Se- at 79.95 g/mol; (f) Nano-TOF-SIMS positive ion scan with counts for a m/z range of 0 – 100 g/mol; (g) Nano-TOF-SIMS negative ion analysis with emphasis on counts of C7H7+ at 91 g/mol.
(a)
(b)
(c)
0
50
150
79.80
79.85
79.90
79.95
80.00
(d)
(e)
0
50
150
Mass [m/z]
90.0
90.5
91.0
91.5
(f)
(g)
Negative ion scan
Negative ion scan, Se-
Positive ion scan
Positive ion scan, C7H7+
Microscope image
1453 cm-1 map
Full spectra analysis
O-PTIR
TOF-SIMS
100
Chart: 
Wavenumber (cm-1)
Confirmed Se-PS-MNPs peaks
Unconfirmed Se-PS-MNPs peaks
100

## Slide 5
0.1 ppm exposure 0.7% w/w c-Se-PS-MNPs
Figure S12. Additional O-PTIR and Nano-TOF-SIMS information for Figure 5. (a) Original 10x O-PTIR microscope image of a histological slice of a Daphnia magna exposed to 0.1 ppm 0.7% w/w Se-PS-MNPs. Emphasis is put on a section of the digestive tract. Red dotted square indicates location of the analysis; (b) O-PTIR mapping of a 96 x 85 µm region of the exposed D. magna at the wavenumber 1452 cm-1 aromatic C-H bending identifiable in polystyrene with point analysis shown by the red crosses at 30 random locations with intensities above 7 mV, with color bar shown on the right side of the image. Mapping done with a scan rate of 100 µm/s at a resolution of 0.2 µm/point with a probe power of 3% and an IR power of 17%; (c) Individual O-PTIR spectrum for each red cross in b) with small circles indicating the presence of identified Se-PS-MNPs by the sharp peaks at 1491 cm-1 and 1453 cm-1 and small triangles indicating non-confirmation of the presence of Se-PS-MNPs; (d) Nano-TOF-SIMS negative ion scan with counts for a m/z range of 0 – 100 g/mol; (e) Nano-TOF-SIMS negative ion analysis with emphasis on counts of Se- at 79.95 g/mol; (f) Nano-TOF-SIMS positive ion scan with counts for a m/z range of 0 – 100 g/mol; (g) Nano-TOF-SIMS negative ion analysis with emphasis on counts of C7H7+ at 91 g/mol.
(a)
(b)
(c)
0
50
150
79.80
79.85
79.90
79.95
80.00
(d)
(e)
0
50
150
Mass [m/z]
90.0
90.5
91.0
91.5
(f)
(g)
Negative ion scan
Negative ion scan, Se-
Positive ion scan
Positive ion scan, C7H7+
Microscope image
1453 cm-1 map
Full spectra analysis
O-PTIR
TOF-SIMS
Confirmed Se-PS-MNPs peaks
Unconfirmed Se-PS-MNPs peaks
Chart: 
100
Wavenumber (cm-1)
100

## Slide 6
1 ppm exposure 0.7% w/w Se-PS-NPs
Figure S13. Additional O-PTIR and Nano-TOF-SIMS information for Figure 5. (a) Original 10x O-PTIR microscope image of a histological slice of a Daphnia magna exposed to 1 ppm 0.7% w/w Se-PS-NPs. Emphasis is put on a section of the digestive tract. Red dotted square indicates location of the analysis; (b) O-PTIR mapping of a 96 x 85 µm region of the exposed D. magna at the wavenumber 1453 cm-1 aromatic C-H bending identifiable in polystyrene with point analysis shown by the red crosses at 30 random locations with intensities above 7 mV, with color bar shown on the right side of the image. Mapping done with a scan rate of 100 µm/s at a resolution of 0.1 µm/point with a probe power of 3% and an IR power of 17%; (c) Individual O-PTIR spectrum for each red cross in b) with small circles indicating the presence of identified Se-PS-MNPs by the sharp peaks at 1491 cm-1 and 1453 cm-1 and small triangles indicating non-confirmation of the presence of Se-PS-MNPs; (d) Nano-TOF-SIMS negative ion scan with counts for a m/z range of 0 – 100 g/mol; (e) Nano-TOF-SIMS negative ion analysis with emphasis on counts of Se- at 79.95 g/mol; (f) Nano-TOF-SIMS positive ion scan with counts for a m/z range of 0 – 100 g/mol; (g) Nano-TOF-SIMS negative ion analysis with emphasis on counts of C7H7+ at 91 g/mol.
(a)
(b)
(c)
0
50
150
78.80
78.85
78.90
78.95
79.00
(d)
(e)
0
50
150
Mass [m/z]
90.0
90.5
91.0
91.5
(f)
(g)
Negative ion scan
Negative ion scan, Se-
Positive ion scan
Positive ion scan, C7H7+
Microscope image
1453 cm-1 map
Full spectra analysis
O-PTIR
TOF-SIMS
100
Chart: 
Wavenumber (cm-1)
Confirmed Se-PS-NPs peaks
Unconfirmed Se-PS-NPs peaks
100

## Slide 7
0.1 ppm exposure 0.7% w/w Se-PS-NPs
Figure S14. Additional O-PTIR and Nano-TOF-SIMS information for Figure 5. (a) Original 10x O-PTIR microscope image of a histological slice of a Daphnia magna exposed to 0.1 ppm 0.7% w/w Se-PS-NPs. Emphasis is put on a section of the digestive tract. Red dotted square indicates location of the analysis; (b) O-PTIR mapping of a 96 x 85 µm region of the exposed D. magna at the wavenumber 1453 cm-1 aromatic C-H bending identifiable in polystyrene with point analysis shown by the red crosses at 30 random locations with intensities above 7 mV, with color bar shown on the right side of the image. Mapping done with a scan rate of 100 µm/s at a resolution of 0.1 µm/point with a probe power of 3% and an IR power of 17%; (c) Individual O-PTIR spectrum for each red cross in b) with small circles indicating the presence of identified Se-PS-MNPs by the sharp peaks at 1491 cm-1 and 1453 cm-1 and small triangles indicating non-confirmation of the presence of Se-PS-MNPs; (d) Nano-TOF-SIMS negative ion scan with counts for a m/z range of 0 – 100 g/mol; (e) Nano-TOF-SIMS negative ion analysis with emphasis on counts of Se- at 79.95 g/mol; (f) Nano-TOF-SIMS positive ion scan with counts for a m/z range of 0 – 100 g/mol; (g) Nano-TOF-SIMS negative ion analysis with emphasis on counts of C7H7+ at 91 g/mol.
(a)
(b)
Wavenumber (cm-1)
(c)
0
50
150
79.80
79.85
79.90
79.95
80.00
(d)
(e)
0
50
150
Mass [m/z]
90.0
90.5
91.0
91.5
(f)
(g)
Negative ion scan
Negative ion scan, Se-
Positive ion scan
Positive ion scan, C7H7+
Microscope image
1453 cm-1 map
Full spectra analysis
O-PTIR
TOF-SIMS
100
Chart: 
Confirmed Se-PS-NPs peaks
Unconfirmed Se-PS-NPs peaks
100