## Slide 1: SI Figures

## Slide 2
Chart: 
Chart: 
Chart: 
Chart: 
(a)
(b)
Chemical shift δ (ppm)
Chemical shift δ (ppm)
Se-M ethanol recrystallization
Se-M ethanol + 1x methanol recrystallization
(c)
(d)
impurities
impurities
Figure S1. Raw 8-scans 1H-NMR for different stages of p-phenylselenomethylstyrene (Se-M) purification process. (a) Overall 1H-NMR spectra for Se-M after ethanol recrystallization; (b) Emphasis put on impurities with smaller doublets of doublets (dd) at 5.3 and 5.7 ppm indicates presence of vinyl species such as bis(p-vinylbenzyl) selenide (s) at 4.55 ppm and p-vinylbenzyl alcohol (s) at 4.65 ppm. Ether species (s) at 3.70 ppm such as p-vinylbenzyl methyl ether may have been formed during the synthesis; (c) Overall 1H-NMR spectra for Se-M after ethanol and 1x methanol recrystallization; (d) Emphasis put on impurities with smaller dd at 5.3 and 5.7 ppm. Peaks reduced intensity suggests effective reduction of impurities.

## Slide 3
Chart: 
0.25 % w/w R1
0.25 % w/w R2
0.25 % w/w R3
0.7 % w/w R1
0.7 % w/w R2
0.7 % w/w R3
2.7 % w/w R1
2.7 % w/w R2
2.7 % w/w R3
Chart: 
4.05 ppm (s)
4.05 ppm (s)
Chemical shift δ (ppm)
SI Figure 2B. Additional H-NMR data on triplicates (R1-R2-R3) for different Se-to-polymer ratios determined by XPS (0.3%, 0.7%, 2.3% w/w). Emphasis in purple box was put on the chemical shift around 4.05 ppm, indicates singlet corresponding to 2H on R-Se-CH2-R. Increased ratio increased intensity.
(a)
(b)
Figure S2. Additional 1H-NMR and XPS data on triplicates (R1, R2, R3) for different Se-to-polymer ratios determined by XPS. (a) 1H-NMR spectra for individual replicates and values provided on spectra are XPS data. Average XPS Se-to-polymer weight ratio compiles to 0.25 ± 0.02% w/w for a feed ratio of 0.5% w/w, 0.72 ± 0.10% w/w for a feed ratio of 1.0% w/w and 2.6 ± 0.18% w/w for a feed ratio of 3.0% w/w; (b) Emphasis in purple box was put on the chemical shift around 4.05 ppm, indicates singlet corresponding to 2H on R-Se-CH2-R.

## Slide 4
Chart: 
Chart: 
| 1461 | 1463 | 1465 | 1467 | 1469 | 1471 | 1473 | 1475 | 1477 | 1479 | 1481 | 1483 | 1485 | 1487 | 1489 | 1491 | 1493 | 1495 | 1497 | 1499 | 1501 | 1503 | 1505 | 1507 | 1509 | 1511 | 1513 | 1515 | 1517 | 1519 | 1521
D_1/O-PTIR (mV) [] | 8.1048 | 8.0746 | 8.0587 | 8.056 | 8.0547 | 8.0546 | 8.0499 | 8.0521 | 8.0613 | 8.0714 | 8.082 | 8.1134 | 8.1564 | 8.2357 | 8.3676 | 8.7625 | 8.9141 | 8.7673 | 8.4513 | 8.2249 | 8.1294 | 8.0823 | 8.0613 | 8.0386 | 8.0382 | 8.0461 | 8.0371 | 8.0354 | 8.0232 | 8.015 | 8.0142
D_2/O-PTIR (mV) [] | 7.9221 | 7.8956 | 7.866 | 7.8665 | 7.8643 | 7.8522 | 7.8581 | 7.8565 | 7.8715 | 7.8929 | 7.9099 | 7.9264 | 7.9721 | 8.0724 | 8.237 | 8.6996 | 8.8386 | 8.6648 | 8.3277 | 8.0602 | 7.9205 | 7.8719 | 7.8199 | 7.8193 | 7.832 | 7.8198 | 7.8105 | 7.8089 | 7.8077 | 7.809 | 7.8097
D_3/O-PTIR (mV) [] | 7.7178 | 7.6874 | 7.6629 | 7.6404 | 7.6329 | 7.6156 | 7.6195 | 7.6185 | 7.6162 | 7.6188 | 7.6402 | 7.6778 | 7.7343 | 7.8039 | 7.9688 | 8.3721 | 8.4807 | 8.34 | 8.0329 | 7.7753 | 7.6773 | 7.647 | 7.591 | 7.5993 | 7.611 | 7.5958 | 7.6005 | 7.6145 | 7.5788 | 7.5663 | 7.5812
D_4/O-PTIR (mV) [] | 7.4658 | 7.4464 | 7.4349 | 7.4344 | 7.4317 | 7.4281 | 7.4267 | 7.4287 | 7.4342 | 7.4358 | 7.4395 | 7.4545 | 7.4853 | 7.5542 | 7.6817 | 8.0657 | 8.2423 | 8.1003 | 7.7711 | 7.5514 | 7.471 | 7.4406 | 7.422 | 7.416 | 7.4129 | 7.4137 | 7.4087 | 7.4016 | 7.3996 | 7.4018 | 7.4043
D_5/O-PTIR (mV) [] | 7.3031 | 7.2678 | 7.2428 | 7.2477 | 7.2476 | 7.2324 | 7.231 | 7.2379 | 7.2589 | 7.2624 | 7.2796 | 7.3139 | 7.368 | 7.4628 | 7.6312 | 8.0686 | 8.1913 | 8.0085 | 7.6703 | 7.4231 | 7.3143 | 7.2583 | 7.2267 | 7.215 | 7.2247 | 7.2139 | 7.2032 | 7.1901 | 7.1915 | 7.1974 | 7.1859
D_6/O-PTIR (mV) [] | 7.1086 | 7.0743 | 7.0623 | 7.0737 | 7.0614 | 7.0357 | 7.0208 | 7.0395 | 7.0549 | 7.0955 | 7.0777 | 7.1144 | 7.1929 | 7.2849 | 7.5003 | 8.0409 | 8.192 | 7.9987 | 7.5416 | 7.25 | 7.1342 | 7.0565 | 7.0156 | 7.0142 | 7.0109 | 7.036 | 6.9924 | 6.9677 | 6.9702 | 6.9413 | 7.0037
D_7/O-PTIR (mV) [] | 6.9433 | 6.9126 | 6.8761 | 6.8763 | 6.8747 | 6.8602 | 6.8644 | 6.8748 | 6.8855 | 6.8951 | 6.9073 | 6.9495 | 6.9987 | 7.0924 | 7.2752 | 7.7353 | 7.8771 | 7.7014 | 7.3562 | 7.0793 | 6.9339 | 6.8631 | 6.8164 | 6.7858 | 6.8148 | 6.829 | 6.8433 | 6.8249 | 6.8006 | 6.8057 | 6.7811
D_8/O-PTIR (mV) [] | 6.6271 | 6.6065 | 6.6111 | 6.5979 | 6.6076 | 6.6059 | 6.6239 | 6.5977 | 6.5982 | 6.6147 | 6.6117 | 6.6334 | 6.6207 | 6.623 | 6.6829 | 7.0871 | 7.325 | 7.1799 | 6.8089 | 6.6112 | 6.5811 | 6.5978 | 6.6306 | 6.6297 | 6.6383 | 6.6146 | 6.6522 | 6.671 | 6.636 | 6.6022 | 6.6303
D_9/O-PTIR (mV) [] | 6.5558 | 6.5172 | 6.4907 | 6.4878 | 6.4828 | 6.4766 | 6.4764 | 6.4826 | 6.4948 | 6.4985 | 6.5011 | 6.5527 | 6.6207 | 6.734 | 6.9373 | 7.3512 | 7.4495 | 7.2766 | 6.9494 | 6.6799 | 6.5454 | 6.4946 | 6.4547 | 6.4336 | 6.425 | 6.4141 | 6.4251 | 6.432 | 6.4279 | 6.4216 | 6.4143
D_10/O-PTIR (mV) [] | 6.3691 | 6.3261 | 6.2832 | 6.2774 | 6.2901 | 6.2939 | 6.2803 | 6.2689 | 6.2748 | 6.2827 | 6.3158 | 6.3952 | 6.456 | 6.5452 | 6.7315 | 7.1803 | 7.248 | 7.0579 | 6.7488 | 6.5062 | 6.3837 | 6.3363 | 6.2925 | 6.2182 | 6.2109 | 6.2338 | 6.2211 | 6.2226 | 6.225 | 6.2152 | 6.2284
E1/O-PTIR (mV) [] | 5.1981 | 5.1728 | 5.1398 | 5.127 | 5.1296 | 5.1201 | 5.1164 | 5.1372 | 5.1501 | 5.13 | 5.1454 | 5.2111 | 5.2795 | 5.3781 | 5.5802 | 5.8907 | 5.9551 | 5.7988 | 5.5122 | 5.3133 | 5.21 | 5.1621 | 5.1215 | 5.0863 | 5.0924 | 5.0893 | 5.0727 | 5.0459 | 5.0384 | 5.0228 | 5.0161
E2/O-PTIR (mV) [] | 5.0277 | 4.9771 | 4.9467 | 4.9436 | 4.9115 | 4.8913 | 4.933 | 4.9321 | 4.9267 | 4.9305 | 4.955 | 5.0184 | 5.1051 | 5.2057 | 5.3949 | 5.8271 | 5.9437 | 5.8248 | 5.4852 | 5.1779 | 5.0233 | 4.9559 | 4.8941 | 4.8303 | 4.8062 | 4.8231 | 4.8209 | 4.8018 | 4.836 | 4.8394 | 4.8434
1492 cm-1
1492 cm-1
Wavenumber (cm-1)
R1
R2
R3
0.25% w/w Se-PS
(a)
(b)
(c)
Figure S3. (a) Raw O-PTIR data on triplicates (R1, R2, R3) at 10 different locations for 0.25% w/w Se-PS; (b) Emphasis in green box was put on the wavenumber around 1492 cm-1, where indistinct peaks appear at 1480 cm-1 (para-disubstituted phenyl ring) and 1510 cm-1 (monosubstituted -SePh phenyl ring); (c) O-PTIR microscope images of 0.25% w/w Se-PS at 10x magnification with locations for spectra acquisitions indicated as small red squares.

## Slide 5
Chart: 
| 1461 | 1463 | 1465 | 1467 | 1469 | 1471 | 1473 | 1475 | 1477 | 1479 | 1481 | 1483 | 1485 | 1487 | 1489 | 1491 | 1493 | 1495 | 1497 | 1499 | 1501 | 1503 | 1505 | 1507 | 1509 | 1511 | 1513 | 1515 | 1517 | 1519 | 1521
1G_10/O-PTIR (mV) [] | 8.1498 | 8.1253 | 8.1081 | 8.1008 | 8.1014 | 8.0966 | 8.1015 | 8.1148 | 8.1256 | 8.1312 | 8.1405 | 8.1746 | 8.229 | 8.3167 | 8.4567 | 8.8274 | 8.9242 | 8.7321 | 8.4464 | 8.2489 | 8.1548 | 8.1108 | 8.0898 | 8.0677 | 8.0642 | 8.0639 | 8.0554 | 8.0413 | 8.0246 | 8.0149 | 8.011
1G_11/O-PTIR (mV) [] | 7.9243 | 7.9097 | 7.8734 | 7.865 | 7.8703 | 7.8602 | 7.8534 | 7.8856 | 7.8998 | 7.9127 | 7.904 | 7.9686 | 8.0092 | 8.1107 | 8.2368 | 8.3361 | 8.2547 | 8.1557 | 8.0469 | 7.9736 | 7.9098 | 7.8511 | 7.8069 | 7.7765 | 7.8311 | 7.8181 | 7.8156 | 7.8036 | 7.7257 | 7.7371 | 7.7115
1G_12/O-PTIR (mV) [] | 7.6986 | 7.6588 | 7.6477 | 7.6493 | 7.6904 | 7.6851 | 7.6973 | 7.6962 | 7.7093 | 7.7198 | 7.7159 | 7.714 | 7.7721 | 7.8915 | 8.105 | 8.6171 | 8.7526 | 8.5015 | 8.1313 | 7.8516 | 7.7089 | 7.698 | 7.7266 | 7.7097 | 7.618 | 7.6963 | 7.6914 | 7.6745 | 7.647 | 7.7009 | 7.6367
1G_13/O-PTIR (mV) [] | 7.5454 | 7.4876 | 7.4843 | 7.486 | 7.4721 | 7.4855 | 7.4758 | 7.4916 | 7.5308 | 7.5238 | 7.53 | 7.5724 | 7.6174 | 7.711 | 7.9493 | 8.3364 | 8.3412 | 8.1794 | 7.902 | 7.691 | 7.5802 | 7.5328 | 7.4882 | 7.5169 | 7.5105 | 7.452 | 7.4202 | 7.4141 | 7.365 | 7.4035 | 7.4531
1G_3/O-PTIR (mV) [] | 7.2454 | 7.2256 | 7.2351 | 7.2409 | 7.2263 | 7.2187 | 7.2295 | 7.2291 | 7.2364 | 7.242 | 7.2545 | 7.2663 | 7.2951 | 7.3628 | 7.5122 | 7.887 | 7.9427 | 7.7848 | 7.5144 | 7.32 | 7.2604 | 7.2406 | 7.2179 | 7.1784 | 7.2033 | 7.2163 | 7.2085 | 7.2142 | 7.1986 | 7.1987 | 7.1942
1G_5/O-PTIR (mV) [] | 7.0456 | 7.0221 | 7.0065 | 7.0106 | 7.0031 | 6.9951 | 6.9888 | 7.0048 | 7.013 | 7.0156 | 7.0165 | 7.0399 | 7.0604 | 7.1016 | 7.213 | 7.5806 | 7.7052 | 7.5891 | 7.2883 | 7.0938 | 7.0318 | 7.012 | 7.005 | 6.9773 | 6.9821 | 6.9965 | 6.997 | 7.0046 | 6.9973 | 7 | 7.0004
1G_6/O-PTIR (mV) [] | 6.8736 | 6.8729 | 6.8584 | 6.842 | 6.8363 | 6.8416 | 6.8508 | 6.8452 | 6.8406 | 6.832 | 6.8491 | 6.8874 | 6.9138 | 6.9648 | 7.0466 | 7.2947 | 7.3186 | 7.1431 | 6.9634 | 6.9124 | 6.8868 | 6.8646 | 6.8433 | 6.8676 | 6.877 | 6.8569 | 6.8479 | 6.8191 | 6.8036 | 6.8365 | 6.8474
1G_7/O-PTIR (mV) [] | 6.7451 | 6.73 | 6.7211 | 6.7072 | 6.6991 | 6.6887 | 6.6943 | 6.7118 | 6.7233 | 6.7311 | 6.7456 | 6.7768 | 6.8257 | 6.9049 | 7.0129 | 7.2907 | 7.417 | 7.2841 | 7.0599 | 6.8877 | 6.7875 | 6.736 | 6.6966 | 6.6656 | 6.6738 | 6.6799 | 6.671 | 6.6551 | 6.6586 | 6.6448 | 6.6279
1G_8/O-PTIR (mV) [] | 6.5693 | 6.5367 | 6.5175 | 6.5069 | 6.5047 | 6.5083 | 6.5123 | 6.5136 | 6.5218 | 6.529 | 6.5403 | 6.5897 | 6.6544 | 6.7497 | 6.8745 | 7.257 | 7.3166 | 7.0644 | 6.7919 | 6.694 | 6.6041 | 6.5558 | 6.5238 | 6.5047 | 6.5031 | 6.4994 | 6.4696 | 6.4418 | 6.4244 | 6.4102 | 6.4172
1G_9/O-PTIR (mV) [] | 6.2883 | 6.2753 | 6.2697 | 6.2745 | 6.2764 | 6.2556 | 6.244 | 6.2561 | 6.2792 | 6.2874 | 6.2869 | 6.2721 | 6.2653 | 6.3003 | 6.3784 | 6.9827 | 6.9824 | 6.6429 | 6.443 | 6.3211 | 6.2698 | 6.2463 | 6.2405 | 6.2316 | 6.2297 | 6.2317 | 6.2309 | 6.2266 | 6.2195 | 6.2183 | 6.2098
1H_1/O-PTIR (mV) [] | 5.2109 | 5.1707 | 5.1397 | 5.1238 | 5.1207 | 5.1162 | 5.1127 | 5.1156 | 5.13 | 5.1433 | 5.1642 | 5.2234 | 5.298 | 5.4049 | 5.512 | 5.7088 | 5.8025 | 5.7024 | 5.4946 | 5.2968 | 5.1841 | 5.126 | 5.0938 | 5.0777 | 5.0629 | 5.0591 | 5.0587 | 5.0485 | 5.0382 | 5.0321 | 5.0292
1H_10/O-PTIR (mV) [] | 4.9207 | 4.8829 | 4.8592 | 4.8549 | 4.854 | 4.8437 | 4.8371 | 4.8539 | 4.8668 | 4.874 | 4.8734 | 4.8974 | 4.9593 | 5.037 | 5.2254 | 5.8002 | 5.9515 | 5.7539 | 5.3214 | 5.0472 | 4.9208 | 4.854 | 4.826 | 4.8007 | 4.7949 | 4.8202 | 4.83 | 4.8207 | 4.8213 | 4.8205 | 4.7989
Chart: 
1492 cm-1
1492 cm-1
Wavenumber (cm-1)
R1
R2
R3
0.7% w/w Se-PS
(a)
(b)
(c)
Figure S4. (a) Raw O-PTIR data on triplicates (R1, R2, R3) at 10 different locations for 0.7 w/w Se-PS; (b) Emphasis in green box was put on the wavenumber around 1492 cm-1, where faint peaks appear at 1480 cm-1 (para-disubstituted phenyl ring) and 1510 cm-1 (monosubstituted -SePh phenyl ring); (c) O-PTIR microscope images of 0.7% w/w Se-PS at 10x magnification with locations for spectra acquisitions indicated as small red squares.

## Slide 6
Chart: 
| 1461 | 1463 | 1465 | 1467 | 1469 | 1471 | 1473 | 1475 | 1477 | 1479 | 1481 | 1483 | 1485 | 1487 | 1489 | 1491 | 1493 | 1495 | 1497 | 1499 | 1501 | 1503 | 1505 | 1507 | 1509 | 1511 | 1513 | 1515 | 1517 | 1519 | 1521
3D_1/O-PTIR (mV) [] | 8.0953 | 8.0704 | 8.0544 | 8.0527 | 8.0504 | 8.0459 | 8.0577 | 8.0876 | 8.1135 | 8.1044 | 8.086 | 8.0923 | 8.1231 | 8.1874 | 8.2852 | 8.6723 | 8.8576 | 8.6722 | 8.3637 | 8.1701 | 8.0918 | 8.0581 | 8.0476 | 8.0611 | 8.0682 | 8.0596 | 8.0438 | 8.0222 | 8.016 | 8.0248 | 8.0164
3D_10/O-PTIR (mV) [] | 7.8924 | 7.8489 | 7.8366 | 7.8387 | 7.8519 | 7.8403 | 7.8669 | 7.9216 | 7.941 | 7.9106 | 7.8903 | 7.9027 | 7.958 | 8.0695 | 8.2508 | 8.7536 | 8.9188 | 8.715 | 8.331 | 8.0403 | 7.9039 | 7.8608 | 7.791 | 7.7978 | 7.8708 | 7.8724 | 7.857 | 7.8225 | 7.7928 | 7.7852 | 7.7527
3D_11/O-PTIR (mV) [] | 7.632 | 7.619 | 7.6238 | 7.6114 | 7.6086 | 7.6035 | 7.6051 | 7.6165 | 7.622 | 7.6374 | 7.6282 | 7.6216 | 7.6291 | 7.6548 | 7.7139 | 7.9457 | 8.1852 | 8.0966 | 7.815 | 7.6714 | 7.6314 | 7.6085 | 7.5847 | 7.546 | 7.5746 | 7.5847 | 7.5767 | 7.5554 | 7.5847 | 7.5874 | 7.5812
3D_12/O-PTIR (mV) [] | 7.5736 | 7.5288 | 7.4972 | 7.494 | 7.4884 | 7.4797 | 7.5071 | 7.5576 | 7.6049 | 7.5885 | 7.5584 | 7.5694 | 7.6308 | 7.7519 | 7.981 | 8.4084 | 8.4959 | 8.3292 | 7.9736 | 7.678 | 7.5522 | 7.4967 | 7.4563 | 7.442 | 7.505 | 7.5138 | 7.4842 | 7.4446 | 7.4101 | 7.3971 | 7.3887
3D_13/O-PTIR (mV) [] | 7.3916 | 7.3499 | 7.3199 | 7.3192 | 7.3295 | 7.33 | 7.3415 | 7.3902 | 7.4405 | 7.4298 | 7.3922 | 7.4018 | 7.4594 | 7.5673 | 7.7487 | 8.1187 | 8.2252 | 8.0846 | 7.7721 | 7.5315 | 7.4084 | 7.3517 | 7.3174 | 7.3266 | 7.3804 | 7.3444 | 7.3002 | 7.2833 | 7.2347 | 7.1958 | 7.2009
3D_5/O-PTIR (mV) [] | 7.2074 | 7.1667 | 7.1439 | 7.1362 | 7.1401 | 7.1298 | 7.1577 | 7.2149 | 7.2712 | 7.2455 | 7.2136 | 7.2329 | 7.2735 | 7.3748 | 7.5521 | 7.909 | 8.0133 | 7.894 | 7.604 | 7.3418 | 7.2112 | 7.1579 | 7.1089 | 7.1177 | 7.1646 | 7.1727 | 7.1279 | 7.0808 | 7.0412 | 7.0274 | 7.0342
3D_6/O-PTIR (mV) [] | 6.9679 | 6.9455 | 6.9346 | 6.9273 | 6.9333 | 6.9293 | 6.9595 | 7.0059 | 7.0095 | 6.9894 | 6.9726 | 6.9741 | 7.0101 | 7.0864 | 7.2285 | 7.4381 | 7.4501 | 7.3422 | 7.2071 | 7.0852 | 6.9935 | 6.9401 | 6.8935 | 6.9084 | 6.9404 | 6.9586 | 6.9167 | 6.8762 | 6.8457 | 6.8287 | 6.8001
3D_7/O-PTIR (mV) [] | 6.6639 | 6.6526 | 6.641 | 6.6312 | 6.6345 | 6.6442 | 6.6606 | 6.674 | 6.6761 | 6.6681 | 6.665 | 6.6766 | 6.6977 | 6.745 | 6.8218 | 7.1527 | 7.2908 | 7.0947 | 6.8579 | 6.7077 | 6.6738 | 6.6554 | 6.6309 | 6.6339 | 6.6559 | 6.6503 | 6.6274 | 6.6233 | 6.6195 | 6.6007 | 6.5951
3D_8/O-PTIR (mV) [] | 6.4961 | 6.4736 | 6.4606 | 6.4574 | 6.4602 | 6.4608 | 6.4696 | 6.4882 | 6.5006 | 6.4895 | 6.481 | 6.4916 | 6.5183 | 6.5741 | 6.6858 | 7.0773 | 7.1921 | 6.9977 | 6.7207 | 6.5533 | 6.4871 | 6.4588 | 6.439 | 6.4382 | 6.4587 | 6.456 | 6.4438 | 6.4304 | 6.421 | 6.4159 | 6.4126
3D_9/O-PTIR (mV) [] | 6.2288 | 6.2188 | 6.2142 | 6.2125 | 6.2128 | 6.2121 | 6.2154 | 6.2207 | 6.225 | 6.224 | 6.2233 | 6.2309 | 6.2469 | 6.2733 | 6.3341 | 6.6224 | 6.7071 | 6.569 | 6.3821 | 6.278 | 6.2411 | 6.2257 | 6.2178 | 6.2195 | 6.2221 | 6.2228 | 6.224 | 6.2161 | 6.2072 | 6.2056 | 6.2032
3E_1/O-PTIR (mV) [] | 5.126 | 5.102 | 5.0868 | 5.0826 | 5.0809 | 5.0773 | 5.0965 | 5.1414 | 5.1731 | 5.1586 | 5.1384 | 5.1615 | 5.2284 | 5.3653 | 5.6324 | 5.9527 | 5.8686 | 5.6909 | 5.4252 | 5.2275 | 5.1309 | 5.08 | 5.0551 | 5.0639 | 5.0856 | 5.0878 | 5.0726 | 5.0484 | 5.0204 | 5.0213 | 5.0126
3E_10/O-PTIR (mV) [] | 4.924 | 4.9009 | 4.8888 | 4.8843 | 4.8859 | 4.8864 | 4.9074 | 4.9367 | 4.9511 | 4.937 | 4.9265 | 4.9412 | 4.9781 | 5.0571 | 5.1919 | 5.4955 | 5.4991 | 5.3301 | 5.1282 | 4.9854 | 4.9193 | 4.8903 | 4.8685 | 4.8731 | 4.9025 | 4.9003 | 4.8766 | 4.8575 | 4.8386 | 4.8265 | 4.8164
Chart: 
#REF! | 1
#REF! | 1
1492 cm-1
1492 cm-1
(a)
(b)
(c)
Wavenumber (cm-1)
2.7% w/w Se-PS
R1
R2
R3
Figure S5. (a) Raw O-PTIR data on triplicates (R1-R2-R3) at 10 different locations for 2.7% w/w Se-PS; (b) Emphasis in green box was put on the wavenumber around 1492 cm-1, where faint peaks appear at 1480 cm-1 (para-disubstituted phenyl ring) and 1510 cm-1 (monosubstituted -SePh phenyl ring); (c) O-PTIR microscope images of 2.7% w/w Se-PS at 10x magnification with locations for spectra acquisitions indicated as small red squares.
Notes: Nano-tof and OPTIR images

## Slide 7
Chart: 
Chart: 
Chart: 
c-Se-PS-MNPs size (nm)
c-Se-PS-MNPs size (nm)
c-Se-PS-MNPs size (nm)
Model | Z-average (µm) | PI
0.25% w/w | 1.46 ± 0.98 | 0.80 ± 0.28
0.7% w/w | 1.57 ± 0.64 | 0.62 ± 0.30
2.7% w/w | 1.90 ± 1.07 | 0.96 ± 0.35
0.25% w/w
(a)
(b)
(c)
(d)
2.7% w/w
0.7% w/w
Figure S6. (a) DLS size distribution for triplicates of 0.25% w/w Se-PS-MNPs; (b) DLS size distribution for triplicates of 0.7% w/w Se-PS-MNPs; (c) DLS size distribution for triplicates of 2.7% w/w Se-PS-MNPs; (d) Table shows the combined average particle size (z-average) with standard deviations (SD) and the polydispersity index (PI) with SD. Concentrations in the analysis were 10.0 ± 0.1 ppm pre-determined by weight.

## Slide 8
2.7% w/w
0.7% w/w
0.25% w/w
(a)
(b)
(c)
145x
456x
3974x
Figure S7. Example SEM pictures for 0.25% w/w R3, 0.7% w/w R2 and 2.7% w/w R3 Se-PS-MNPs at different magnifications. (a) SEM pictures at 145x magnification with the scale bar shown for 200 µm at a random location. ImageJ calculated average sizes from the provided images and assuming circular particles for 0.25% w/w R3 was 2.49 ± 1.36 µm, 0.7% w/w R2 was 1.83 ± 0.61 µm, and 2.7% w/w was 2.67 ± 1.47 µm R3; (b) SEM pictures at 456x magnification with the scale bar shown for 100 µm at a random location; (c) SEM pictures at 3976x magnification with the scale bar shown for 10 µm on a section of the coffee ring effect. Presence of bigger particles >20 µm was noticed in all samples.