## Slide 1: 0.7% w/w (1% in theory) Nano TOF SIMS raw maps and distributions
For Figure 5 and Figure S10-S12 defg
10 ppm c-Se-PS-MNPs
1 ppm c-Se-PS-MNPs
0.1 ppm C-Se-PS-MNPs
1 ppm Se-PS-NPs
0.1 ppm Se-PS-NPs
All maps brightness and contrast were adjusted to enhance the brightest spots using the Picture format  Corrections option on Power Point, more correction were done on the official figures PP slides

## Slide 2: 10 ppm c-Se-PS-MNPs

## Slide 3
positive- (1%w/w) -10 (ppm) -B-400 um
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 41150639; Max: 1496; Scale: 100µm
Se - 79.92 (256x256)
Cts: 41419; Max: 7; Scale: 100µm
C7H7 - 91.03 (256x256)
Cts: 77933; Max: 19; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 4
positive- (1%w/w) -10 (ppm) -B-400 um
0
50
100
150
Mass [m/z]
0
1
2
3
4
5
6
7
Counts/1E6
41
95
23
104
123
79
120
97
86
27
157
*25 june 25-spot 1-1-10-400 um-001~pb1.tdc + Ions 400µm 41150639 cts
79.80
79.85
79.90
79.95
80.00
Mass [m/z]
0.0
0.5
1.0
1.5
Counts/1E3
80.0453
*25 june 25-spot 1-1-10-400 um-001~pb1.tdc + Ions 400µm 41150639 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0
1
2
3
4
5
Counts/1E3
90.98
91.94
90.93
91.15
*25 june 25-spot 1-1-10-400 um-001~pb1.tdc + Ions 400µm 41150639 cts
Enter Slide Comments Here

## Slide 5
Negative- (1%w/w) -10 (ppm) -B-400 um
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 92675861; Max: 3701; Scale: 100µm
Se - 79.92 (256x256)
Cts: 13327; Max: 9; Scale: 100µm
C7H7 - 91.03 (256x256)
Cts: 147333; Max: 20; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 6
Negative- (1%w/w) -10 (ppm) -B-400 um
0
50
100
150
Mass [m/z]
0
2
4
6
8
Counts/1E6
13
16
79
42
26
45
59
63
71
69
49
*25 june 25-spot 1-1-10-negative-400 um-002~pb1.tdc - Ions 400µm 92675862 cts
79.80
79.85
79.90
79.95
80.00
Mass [m/z]
0.0
0.2
0.4
0.6
0.8
1.0
1.2
1.4
Counts/1E4
80.0274
80.0205
*25 june 25-spot 1-1-10-negative-400 um-002~pb1.tdc - Ions 400µm 92675862 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0
1
2
3
4
5
6
7
Counts/1E3
90.02
91.98
*25 june 25-spot 1-1-10-negative-400 um-002~pb2.ROI1.tdc - Ions 400µm 21147445 cts

## Slide 7: 1 ppm c-Se-PS-MNPs

## Slide 8
2 Sep 25- 1-1- C-20 um-400 um-negative-second time
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 80062701; Max: 2857; Scale: 100µm
Se - 79.92 (256x256)
Cts: 80319; Max: 15; Scale: 100µm
91.041 (256x256)
Cts: 9857; Max: 4; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 9
2 Sep 25- 1-1-C-20 um-400 um-nagative-002-good
0
20
40
60
80
Mass [m/z]
0.0
0.2
0.4
0.6
0.8
1.0
Counts/1E7
1
13
79
26
17
41
42
63
59
25
16
12
*2 Sep 25-1-1-C-20 um-100-negative-006.tdc - Ions 400µm 80062701 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0
2
4
6
8
Counts/1E3
*2 Sep 25-1-1-C-20 um-100-negative-006.tdc - Ions 400µm 80062701 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0.0
0.5
1.0
1.5
Counts/1E4
91.92
*2 Sep 25-1-1-C-20 um-100-negative-006.tdc - Ions 400µm 80062701 cts
Enter Slide Comments Here

## Slide 10: 0.1 ppm c-Se-PS-MNPs

## Slide 11
3 Sep 25- 0.1-1C-20um-400 um-positive
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 32591190; Max: 921; Scale: 100µm
Se - 79.92 (256x256)
Cts: 2022; Max: 2; Scale: 100µm
91.041 (256x256)
Cts: 429; Max: 2; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 12
0
20
40
60
80
Mass [m/z]
0
1
2
3
4
5
6
Counts/1E6
41
23
95
28
78
79
97
40
29
24
1
*3 Sep 25-1-0.1-C-20 um-400-positive-after puttering 30 se-005.tdc + Ions 400µm 32591190 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
2.5
Counts/1E3
79.9767
*3 Sep 25-1-0.1-C-20 um-400-positive-after puttering 30 se-005.tdc + Ions 400µm 32591190 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0.0
0.2
0.4
0.6
0.8
1.0
1.2
1.4
1.6
Counts/1E3
90.94
91.05
91.07
91.01
*3 Sep 25-1-0.1-C-20 um-400-positive-after puttering 30 se-005.tdc + Ions 400µm 32591190 cts
Enter Slide Comments Here
3 Sep 25- 0.1-1C-20um-400 um-positive

## Slide 13
3 Sep 25- 1-0.1- C-20 um-400 um-negative-002-good
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 95329110; Max: 3115; Scale: 100µm
Se - 79.96 (256x256)
Cts: 21119; Max: 8; Scale: 100µm
91.041 (256x256)
Cts: 11872; Max: 6; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 14
0
20
40
60
80
Mass [m/z]
0
1
2
3
4
5
6
Counts/1E6
1
16
25
17
13
26
12
24
41
49
42
50
*3 Sep 25-1-0.1-C-20 um-400-negative-after puttering 30 se-003.tdc - Ions 400µm 81286519 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0
100
200
300
400
500
600
700
Counts
*3 Sep 25-1-0.1-C-20 um-400-negative-after puttering 30 se-003.tdc - Ions 400µm 81286519 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
2.5
Counts/1E4
91.86
91.87
*3 Sep 25-1-0.1-C-20 um-400-negative-after puttering 30 se-003.tdc - Ions 400µm 81286519 cts
Enter Slide Comments Here
3 sept-0.1-1 -C 20 um-after sputtering 30 s-400 um-negative-009

## Slide 15: 1 ppm Se-PS-NPs

## Slide 16
2 sep 25-1-1- 400 um-positive-
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 36071897; Max: 907; Scale: 100µm
Se - 79.91 (256x256)
Cts: 92648; Max: 9; Scale: 100µm
91.041 (256x256)
Cts: 1916; Max: 3; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 17
2 Sep 25-sample (1-1)-400um-poitive
0
20
40
60
80
Mass [m/z]
0
2
4
6
8
Counts/1E6
41
23
95
28
78
40
79
24
97
94
*2 Sep 25- 1-1- NPs-400 um-positive-005.tdc + Ions 400µm 36071896 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
2.5
3.0
Counts/1E3
*2 Sep 25- 1-1- NPs-400 um-positive-005.tdc + Ions 400µm 36071896 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
Counts/1E3
90.96
91.08
91.09
*2 Sep 25- 1-1- NPs-400 um-positive-005.tdc + Ions 400µm 36071896 cts
Enter Slide Comments Here

## Slide 18
2 sep 25-1-1-negative-400 um
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 47655321; Max: 1193; Scale: 100µm
Se - 79.97 (256x256)
Cts: 69473; Max: 9; Scale: 100µm
91.041 (256x256)
Cts: 13011; Max: 5; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 19
2 sep 25-1-1 negative-400 um
0
20
40
60
80
Mass [m/z]
0
1
2
3
4
5
6
Counts/1E6
1
79
13
25
16
17
41
43
59
26
12
71
*2 Sep 25- 1-1- NPs-400 um-negative-005.tdc - Ions 400µm 47655321 cts
78.80
78.85
78.90
78.95
Mass [m/z]
0
1
2
3
4
5
6
Counts/1E4
*2 Sep 25- 1-1- NPs-400 um-negative-005.tdc - Ions 400µm 47655321 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0
1
2
3
4
Counts/1E3
91.97
90.02
91.09
91.13
91.11
90.20
90.23
*2 Sep 25- 1-1- NPs-400 um-negative-005.tdc - Ions 400µm 47655321 cts
Enter Slide Comments Here

## Slide 20: 0.1 ppm Se-PS-NPs

## Slide 21
2 Sep 25- 1-0.1- NPs-400 um-postive-002-good
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 20735271; Max: 575; Scale: 100µm
Se - 79.97 (256x256)
Cts: 11029; Max: 4; Scale: 100µm
91.055 (256x256)
Cts: 38217; Max: 11; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 22
2 Sep 25- 1-0.1- NPs-400 um-postive-002-good
0
20
40
60
80
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
2.5
3.0
Counts/1E6
23
41
97
95
29
28
79
55
27
43
81
*2 Sep 25- 1-0.1- NPs-400 um-postive-002.tdc + Ions 400µm 20735271 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0
100
200
300
400
Counts
*2 Sep 25- 1-0.1- NPs-400 um-postive-002.tdc + Ions 400µm 20735271 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0.0
0.5
1.0
1.5
2.0
Counts/1E3
91.93
91.92
90.93
90.97
90.03
90.04
*2 Sep 25- 1-0.1- NPs-400 um-postive-002.tdc + Ions 400µm 20735271 cts
Enter Slide Comments Here

## Slide 23
2 Sep 25- 1-0.1- NPs-400 um-negative-
+ Ions, xxx µm analysis area (xxx µm scale bar)
Total_Ion (256x256)
Cts: 43763782; Max: 1915; Scale: 100µm
79.930 (256x256)
Cts: 13478; Max: 6; Scale: 100µm
91.055 (256x256)
Cts: 39615; Max: 24; Scale: 100µm
OVERLAY
Enter Slide Comments Here

## Slide 24
2 Sep 25- 1-0.1- NPs-400 um-nagative-002-good
0
20
40
60
80
Mass [m/z]
0
1
2
3
4
5
6
Counts/1E6
26
1
25
17
42
13
12
24
91
60
50
*2 Sep 25- 1-0.1- NPs-400 um-negative-after 20 s sputtering-002.tdc - Ions 400µm 43763782 cts
79.80
79.85
79.90
79.95
Mass [m/z]
0
5
10
15
20
25
30
35
Counts
*2 Sep 25- 1-0.1- NPs-400 um-negative-after 20 s sputtering-002.tdc - Ions 400µm 43763782 cts
90.0
90.5
91.0
91.5
Mass [m/z]
0
1
2
3
4
Counts/1E4
90.09
*2 Sep 25- 1-0.1- NPs-400 um-negative-after 20 s sputtering-002.tdc - Ions 400µm 43763782 cts
Enter Slide Comments Here